## Slide 1: WORKSHOP on In-Situ Compressive Strength of Concrete Structure by Sigma Test & Research Centre Delhi

## Slide 2
The Traditional Cube test measures the potential compressive strength of a given mix after 28 days , when the concrete under ideal laboratory conditions is compacted and cured in water at 27° Celsius.
Need for IN-PLACE Strength Testing During Construction

## Slide 3: Strength of Structure Depends
Transportation of concrete
Pumping
Casting
Compaction
Effective curing
Maturity developed on-site

## Slide 4: In-Place Strength
Evaluation of in-place strength as per existing practice
Testing Methods | Limitations
Core drilling | Destructive Test, High Measurement Time.
Rebound hammer | High Uncertainty, Measures surface Hardness.
Ultrasonic Pulse Velocity Test | Qualitative Test, Low Coverage.

## Slide 5: Objective Pullout Test (ASTM C 900)
Pullout test of concrete determines the compressive strength of concrete as available at site taking into account all the variables outlined earlier for a direct comparison with the results of standards compression test as measured at the ready-mix plant under ideal laboratory conditions.

## Slide 6: Pullout Test Method
18 mm diameter hole is drilled into the concrete up to 65mm depth.
With the help of special concrete router bit a 25mm diameter slot is made.
An expandable metal washer is placed in a hole and ring is expanded.
The expanded washer is then pulled out of the concrete using the pull out loading system.

## Slide 10
NUT
COILED RING
CONE
Ring Expansion Hardware

## Slide 11
Commercial Test Systems

## Slide 13: Recommended Number Of Tests (as per ASTM C900)
For Slabs
5 Test points for every 465m² of the surface area.
For Columns and Beams
5 Test points for every 115m³ of concrete.
( Vol. of Col.: 300×450×3650 mm = 0.49 cubic meter )

## Slide 14: Applications
To determine a minimum amount of curing needed in cold weather concreting.
For assessing existing structures.
For planning Rehabilitation, Restrengthning work
For estimating concrete strength during construction.

## Slide 15: Correlation
Irrespective of failure theory, pullout strength is related to a fundamental strength parameter of concrete .
There is good correlation between pullout strength and compressive strength .

## Slide 16: Robust Correlation
Not affected by:
Cementitious materials
Water-cement ratio
Age
Air entrainment
Admixtures
Shape or size of aggregate up to 40 mm

## Slide 19
Comparison Between Compressive Strength Test From
Core , CAPO and Schmidt Hammer

## Slide 20
On the spot Results
High Accuracy , Repeatability
Consistent Results
Non Destructive
Helps in Localizing problem
Advantages

## Slide 21: Advantages
“Speed of the overall construction programme can be
Increased if an accurate assessment of the early-age in – situ strength is made because this allows a much faster turn around”.
Dept. of Civil Engineers
The University of Liverpool

## Slide 22
Min of Textile , Government of Chad , Africa
CASE STUDIES

## Slide 23
Samsung India - Sec 102, Noida
700000 Sq. ft. Area
Times of India - Gurgaon
Luxor of International - Noida
Sri Sri Ayurveda - Kotdwar , Uttaranchal
CASE STUDIES

## Slide 24: IS Reference